# Approval Note — Thickness Deficiency, 8-P-1204 E-14

Prepared 2026-09-12 · DRAFT — requires human review and approval

## Summary

Ultrasonic survey of 8-P-1204 E-14 records wall thickness of 5.9 mm against a nominal 8.0 mm after 7.0 years in service.

## Findings

| Location | Observation | Measured | Minimum | Severity |
| --- | --- | --- | --- | --- |
| E-14 | Measured wall thickness 5.9 mm against nominal 8.0 mm; retirement limit 6.4 mm | 5.9 mm | 6.4 mm | critical |

## Calculations

Uniform corrosion rate from thickness loss over time: 0.3 mm/a

expression: (-t_measured + t_nominal)/years

substitute t_nominal = 8.0, t_measured = 5.9, years = 7.0

= 0.300000000000000

= 0.3

0.3 mm/yr uniform loss

Years until measured thickness reaches the retirement limit: 0 (already below retirement limit)

expression: (t_measured - t_minimum)/corrosion_rate

substitute t_measured = 5.9, t_minimum = 6.4, corrosion_rate = 0.29999999999999993

= -1.66666666666667

= -1.66667

Measured thickness is already below the retirement limit, so no service life remains. This is a present deficiency, not a future one.

## Recommendation

Measured thickness at E-14 is below the stated retirement limit. Recommend derating or replacing the affected spool before the next run, raised as a work order under management of change.

Generated on-premise by PRAHARI. No data left the organisation's perimeter in producing this document.